ANALYSIS of COAL:

Furnace temperature 1350°C

Sample weight around 300mg, depending on the sensitivity of the analyser and on the C, H and S content of the sample.

The sample weight should not be higher than 500mg.

The sample should be put into the front part of the combustion boat. The 	combustion boat is pushed directly into the hot zone up to the boat stop after pressing “START”. See 2.3.

Usually, no accelerators are needed. Only in exceptional cases, when the sample contains pyrites, the furnace temperature has to be set at 1500°C or approx. 300mg of iron phosphate have to be spread upon the sample.

There are two different types of combustion boats available:

Due to the front shape of the combustion boat type 2, it should be carefully pushed up to the boat stop, otherwise it may slide into the boat stop. Stop pushing as soon as the boat stop is reached.

The combustion boat (1) is reusable (10, 20, 30 analyses or more).

The combustion boat (2) can only be used once