## Applications

ANALYSIS of COAL.

Furnace temperature 1350°C.

Sample weight around 300mg, depending on the sensitivity of the analyser and on the C and S content of the sample. The sample weight should not be higher than 500mg.

Usually, no accelerators are needed. Only in exceptional cases, when the sample contains pyrites, the furnace temperature has to be set at 1500°C or approx. 300mg of iron phosphate have to be spread upon the sample.

GRAPHITE ANALYSIS.

Analysers with a range of 100% C can be calibrated with graphite.

Any furnace temperature over 1000 °C is sufficient.

Sample weight approx. 250 mg.

ANALYSIS of CALCIUM CARBONATE.

This can be used for calibration in the range of 12% C.

Depending on the sensitivity of the IR-cell, the weight can be between 100mg and 500mg.

Any furnace temperature over 800 °C is high enough.

LIMESTONE ANALYSIS.

The furnace temperature 1250 °C or higher.

Calibrate with calcium carbonate of 12% C.

The usual weight is 300mg.

ANALYSIS OF WOOD.

Adjust the furnace temperature to 1300 °C.

Take 350 mg of sample.

Set the minimum analysis time to 50 s.

Set the comparator level to 150.