OFFER
ELTRA CHS-500

Analyser with resistance furnace for carbon, hydrogen and sulfur in coal and coke (complies to the specifications of the standards ISO-10694, ASTM E1915-97, D-1552, D-4239, D-5016, D-1619, DIN EN13137, PN-93 G-04514/17.) and consisting of:

- High temperature furnace up to 1550°C with a 200mm long hot zone and a resolution of 1°C

- Gas flow circulation system complete with electronic flow control, flow displays, pressure gauge, pump, gas cleaning traps

- High-tech infrared cells with solid-state infrared detectors, interference filters and auto-zero and auto-range adjustment.

- Microcontroller

- Electronic balance with 0.0001 g resolution

- PC with CEL 2.6 GHz, 40 GB HDD, 256 MB RAM, Windows XP, CD-ROM, 3.5” drive, keyboard, mouse and 19” TFT-monitor.

- Analysis software for Windows XP with multipoint calibration, automatic linearity correction, applications memory, export to Excel and with universal LIMS export.

- Set of consumables for 500 analyses consisting of: 500 Disposable boats, 50 Re-usable boats, 454 g Anhydrone (magnesium perchlorate), 250 g Sodium hydroxide, 50 g Glass wool.

- Thre calibration materials

- Set of accessories

# CHS-500 SPECIFICATIONS

| MEASURING RANGES |
| --- |
| Carbon Up to 500mg C resp.up to 100% C at 500mg sample 1) | Hydrogen Up to 75mg H resp. up to 15% H at 500mg sample1) | Sulfur Up to 10mg S resp. up to 2% S at 500mg sample 1) |
| Indicating range Up to 100% C 2) | Indicating range Up to 100% H 2) | Indicating range Up to 100% S 2) |
| SENSITIVITY |
| Carbon 5µg C resp. 10 ppm C at 500mg sample | Hydrogen 50µg H resp. 100 ppm H at 500mg sample | Sulfur 1µg S resp. 2 ppm S at 500mg sample |
| ACCURACY |
| Carbon ±50µg C resp. ±100 ppm C at 500mg sample or ±1% of C present | Hydrogen ±100µg H resp. ±200 ppm H at 500mg sample or ±1% of H present | Sulfur 1µg S resp. ±4 ppm S at 500mg sample or ±1% of S present |
| GENERAL SPECIFICATIONS |
| Normal sample weight 200-300mg for coal | Normal analysis time 50 to 180 sec. |
| Furnace temperature Adjustable up to 1550°C | Gas required Oxygen 2 to 4 bar (30 to 60 psi) 3 l/min. |
| Hot Zone Length=200mm, diameter 27=mm | Chemicals CO2 trap sodium hydroxide H2O trap magnesium perchlorate |
| Analyser power requirements 230 V AC ±10% 50/60 Hz 0.33 A / 75 W | Furnace power requirements 230 V AC ±10% 50/60 Hz Maximum heat up current 20 A |
| Weight Analyser Furnace 40kg 36kg | Dimensions Width Height Depth Analyser 55cm (21“) 52cm (20.5“) 60cm (23.5“) Furnace/ 33cm (13“) 52cm (20.5“) 60cm (23.5“) |
| ACCESSORIES |
| Balance 0.0001g to 60 g +/- 0.0001 g Colour InkJet-Printer 4) |

1) Other ranges on request.

2) Possible by reducing the sample weight.

3) Allow 15 cm (6“) access area behind the furnace.

4) Visit our web pages for further details (www.eltragmbh.com/products/accessories.htm).